## Slide 1
VISCOELASTICITY

## Slide 2
VISCOELASTICITY

## Slide 3
VISCOELASTICITY
Experimental Test
Engineering representation of the test
Model
Test results
Characterization the viscoelastic properties of thin hydrogel-based construct for tissue engineering applications

## Slide 4
VISCOELASTICITY

## Slide 5
VISCOELASTICITY
Mechanical deformation and relaxation behavior of a whole Müller (glial) cell (MC) deformed with an optical stretcher.
©2006 by National Academy of Sciences
Yun-Bi Lu et al. PNAS 2006;103:17759-1776

## Slide 6
VISCOELASTICITY
  A viscoelastic material (depending on time, it may be behave either as solid or liquid). At short times it behaves as a solid, at long times it behaves as a liquid
SHORT TIMES
LONG TIMES

## Slide 7
Viscoelastic Materials
TIME is an important variable to study these materials
Time
Frequency
High Frequencies
Short Times
(Solid/Elastic Behavior)
Low Frequencies
Long Times (Fluid/Viscous Behavior)
Could we relate a “rheological parameter” of the material
with its viscoelastic behavior?

## Slide 8
CONCEPT OF VISCOELASTICITY
Maxwell: Viscous flow is the manifestation of the decay of elastically stored energy
Low Energy
High Energy (Stored “elastic” energy)
Low Energy
Deformation
Relaxation (or flow)
Experimental time
texp
Relaxation time
tR

## Slide 9
Viscoelastic Behavior tR is a material property
We should measure viscosity,
We should measure elasticity, G
Elastic Modulus

## Slide 10
VISCOELASTICITY
Is water a viscoelastic Material ?
tR= 10-12 sec

## Slide 11
DEFORMATION DOES NOT
FOLLOW THE FORCE
F
TIME
to
t1
Permanent
Deformation
TIME
L
t1
to
FORCE AND DEFORMATION ARE “ OUT OF PHASE ”
DEFORMATION FOLLOWS THE FORCE
FORCE AND DEFORMATION ARE “ IN PHASE “
F
L
TIME
TIME
F proportional to the Rate of Deformation
" DASHPOT" ~ LIQUID
L
LIQUID
ELASTIC SOLID
L
F proportional
to Deformation
" SPRING " ~ SOLID

## Slide 12
Loss Tangent
Viscoelastic Measurements
Torque bar
Sample
Cup
Bob
Strain 
Stress 
Oscillator
Phase Angle 
Storage Modulus
Loss Modulus

## Slide 13
OSCILLATORY TESTING
Samples are subjected to harmonically varying stress (controlled
stress instrument) or strain (controlled strain instruments)
What are you meaning with this?
Shear Experiment
Sample
h
Plate Displacement versus time
“Shear” Strain versus time

## Slide 14
Shear Experiment
Sample
h
OSCILLATORY TESTING
Oscillation amplitude.
It can be fixed
Frequency = 1/s = Hertz

## Slide 15
Shear Experiment
Sample
h
OSCILLATORY TESTING (Small strain (deformation))
Assume plate separated by 1.5mm (h=1.5mm)
Assume that plate displacement is 0.3mm (Lo=0.3mm)
If Lo = 0.15mm (

## Slide 16
OTHER TYPE OF DEFORMATIONS CAN BE USED
Compression Tension
Engineering Stress and Strain
True Stress and Strain
Bending
Single Cantilever
Double Cantilever
F
d
F
d
b
h
D
Rectangular Section
Circular Section
Rectangular Section
Circular Section
E is the elastic or Young
Modulus
a
a

## Slide 17
CONTROLLED STRESS INSTRUMENTS
Stress Amplitude
(fixed by the user)
Frequency
(fixed by the user)
Input
Output
Strain Amplitude
(measured)
Measured
Measured
Phase Angle
(measured)

## Slide 18
CONTROLLED STRAIN INSTRUMENTS
Input
Output
Strain Amplitude
(fixed by user)
Frequency
(fixed by user)
Stress Amplitude
(measured)
Phase Angle
(measured)
Solid Behavior
Liquid Behavior

## Slide 19
Solid Behavior
Liquid Behavior
Oscillatory Testing
Storage Modulus
Loss Modulus
tan (Phase Angle)

## Slide 20
Oscillatory Testing
Other Viscoelastic Parameters (from Controlled Strain)
Complex Modulus
Complex Viscosity
Dynamic Viscosity
Out of Phase Viscosity

## Slide 21
Oscillatory Testing
Other Viscoelastic Parameters (from Controlled Stress)
Complex Compliance
Storage Compliance
Loss Compliance

## Slide 22
VISCOELATIC MATERIALS
Solid (elastic) and Liquid (viscous) Behavior !!!!
Spring
Dashpot
G

## Slide 23
VISCOELATIC MATERIALS
Maxwell Element
G
What is the stress applied ?
Is the stress the same for the spring and the dashpot ?
What are the strains in the dashpot and the spring ?
Are these strains equals? and how can be calculated ?
How we combine these two elements ?
Answering those questions will
allow us to get a model for the
Maxwell Element
Relaxation Time

## Slide 24
Maxwell Element
G
What happens if a Maxwell Element is oscillated ?
Storage Modulus
Loss Modulus
Solid Behavior

## Slide 25
Biomaterials are more complex than
a single Maxwell
G1
G2
Four Element
Generalized Maxwell
G1
G2
G3
Gn

## Slide 26
Oscillatory Testing
Oscillatory testing is based on inputs (either stress or strain)
that are sine waves ?
How could be sure that strain and stress are harmonically
varying functions (e.g. sine or cosine functions) ?
  See raw data for stress and strain as a function of time
  Sometimes is hard to get raw data
How does data look like ?
Input(it is generally OK)
Output(it is generally jagged)

## Slide 27
Oscillatory Testing
Fourier
Transform
Filtering of
these frequencies
Calculation of
G’
G”
and others

## Slide 28
How could be sure, without seeing the raw data and
the transformation process that both strain and stress
are harmonically varying functions (e.g sine or cosine)?
Concept of Linear Viscoelasticity
The response (rheological) of a material to a harmonic (e.g. sine)
varying function will be also harmonic (sine) if the material
behavior is linear
Linear Material
Behavior
Non-Linear
Material Behavior
Sine Function
Input
Output
Sine Function
Input
Sine Function
Output
?

## Slide 29
How could we determine whether the behavior
of the material is linear?
LINEAR BEHAVIOR
If is increased then is increased by the same extent
For instances, if is increased by 20% then is increased by 20%
So G’ and G” will not change if either or are changed
Linear
Behavior
Non-Linear
Behavior
Stress Sweep Test (Controlled Stress
Strain Sweep Test (Controlled Strain)

## Slide 30
Linear Viscoelastic Region

## Slide 31
OTHER TESTS THAT ARE DONE TO
MEASURE VISCOELASTICITY
Frequency Sweep
Maxwell Element
Generalized Maxwell Element
G1
G2
G3
Gn

## Slide 32
Why do we need to study viscoelastic
materials at different frequencies ?
Solid Material, it is frequency independent
Equations can be used to determine the
relaxation times of materials. Relaxation times are associated with the material molecular structure that provides a good understanding of simple polymeric materials (de Gennes received the Nobel Prize for some of the interpretations and description of molecular behavior). Analysis is harder for food and complex biomaterials.
For a Maxwell Element
Elastic component
Viscous component

## Slide 33
OTHER EXPERIMENTS
Time/Temperature Sweep
Time
tcoagulation
Applications
Cheese production
Gelation reactions
Chemorheology (following
chemical reactions with
changes in rheology of
material
Softening of chocolate due to fat melting
thickening of starch suspensions
due to starch gelatinization
Interaction among components
(proteins and carbohydrates)
Adding Enzyme
(Rennet)
Cheese production
Dough Resting
Frequency constant

## Slide 34
Oscillatory Testing
h
R
At the rim of the top plate the distance
traveled x can be calculated as:
And the strain can be calculated as:
Let’s assume that h=2mm and R=50mm and the
amplitude of the strain is 10%, i.e.
Parallel Plate

## Slide 35
Oscillatory Testing
Cone and Plate
Strain
Cone angle
2-4 degrees
If strain is 10%, i.e.
Concentric Cylinders
Newtonian Fluid
Power-law Fluid

## Slide 36
TIME TO COMPLETE AN OSILLATORY TEST
At least one cycle should be
completed to gather meaningful
data
Time to complete a cycle
depends on frequency
For example for
For

## Slide 37
Effect of Moisture Content and sample
“aging” in rheometer
Wheat Starch at different moisture contents
T=90oC
14%
9.5%
Low moisture contents are preferable on long tests
For high moisture
contents use short tests

## Slide 38
Controlled Stress versus Controlled Strain
Steady shear tests versus oscillatory tests

## Slide 39
Mw=1.7x107- 3.5x108
Potato Starch
Mw=1.5x107- 8.8x107
Wheat Starch
Effect of molecular weight of starch
on rheological properties
32% Glycerol, 0% moisture, 150oC

## Slide 40
X-ray diffraction patterns of wheat and potato starch
8% crystallinity
23% crystallinity

## Slide 41
about 20-23% crystallinity
Amorphous material

## Slide 42
Mw= 5x106
High Amylose Starch
Mw=7.5x107
Waxy Starch
(Amylopectin)

## Slide 43
G’
G”
Effect of Temperature on viscoelastic properties