## Slide 1
VISCOELASTICITY (Chapter 5 – Steffe Book)
Measurements
Steady State Conditions
Elastic Fluid
Non-Elastic Fluid
Because of the elastic behavior normal stresses arise, the easy to measure
is the normal stress pushing the top plate up
Load cell

## Slide 2
Measurements
Unsteady Shear testing
  Oscillatory Testing (small deformation)
  Transient Testing (small and large deformation) 1. Start-up Flow Test
    2. Cessation of Steady Shear Flow
    3. Step Strain (Relaxation experiment)
    4. Creep Test
    5. Recoil Test
Data Generated using Transient Methods
Shear Stress Growth Function
Shear stress decay function
Shear stress relaxation Function or Relaxation Modulus
Shear Creep
Recoil Function (Strain)

## Slide 3
1. Start-up Flow
Large Deborah Number
Elastic Behavior
Small Deborah Number Viscous Behavior
Increasing shear rates
Extremely low shear rate
Non-elastic
fluid

## Slide 4
2. Cessation of Steady Shear Flow

## Slide 5
3. Step Strain or Relaxation Test (not the same than start-up flow)
Relaxation stresses
for materials with
different relaxation
times
Residual stress
Different tR
Relaxation Modulus

## Slide 6
CREEP TEST
t=0
t>0

## Slide 7
4. Creep Test

## Slide 8
5. Recoil Test
Partial Recoil
permanent
deformation
No Recoil
Full Recoil

## Slide 9
How we can describe these very different behaviors?
The best way is to use mechanical analogues or a combination of these
What are mechanical analogues?
Spring – Hooke Law
G
Solid Behavior
Ideal solid or Hookean Material)
Force
deformation
Stronger Spring
Observations
Force is proportional to spring deformation
The material properties (of the spring) are also important
Material Properties (spring) = G
Elastic Modulus
Shear Modulus
Compression
etc it will depend on
test

## Slide 10
Behavior of an Ideal Solid

## Slide 11
Dashpot
LIQUID BEHAVIOR (IDEAL LIQUID or DASHPOT)
Stress is Proportional to the Strain Rate
How would be a curve of strain versus time
when stress is maintained constant?
What are the slopes of the strain versus time
curves ?
Stress Increase

## Slide 12
Behavior of a Ideal Liquid
If a constant stress is applied to an ideal liquid (dashpot), it will deform
and its deformation rate (strain rate) will be constant, in other words
the strain versus time curve will be linear.
What happens when a sudden constant strain is applied to a ideal liquid (dashpot) ?
The stress response will be very complex and is explained schematically below

## Slide 13
Behavior of a Ideal Liquid
After application of a constant stress
Why a straight line?
what is the slope of
the line?
See slide 10

## Slide 14
OTHER MODELS
Maxwell Model (viscoelastic liquid)
G

## Slide 15
Strain of a Maxwell after application of a constant stress
to
t1
t1
to
??
G

## Slide 16
Behavior of the Maxwell Element after
a sudden stress (load) is applied
G
Stress is suddenly applied (time is very short)
Time is t and compared with relaxation time is
much smaller t << tR or t/tR<<1
So
Solid Behavior
Conclusion: For short times and
under a sudden stress the Maxwell
element behaves as a solid element,
i.e. it will deform instantaneously with
a strain

## Slide 17
to
t1
t1
to
??

## Slide 18
G
Behavior of the Maxwell Element after
a sudden stress (load) is applied
At short times only “the elastic part” of the element reacts, the dashpot does not deform
(it acts as a solid bar), so the strain of the
Maxwell element at short times is:
G
What happens a long times?
Long Times
Is the elastic element (spring) deforming any longer ?
What happens with the dashpot?
What is the value of
to is the time at
which deformation
starts

## Slide 19
Behavior of the Maxwell Element after
a sudden stress (load) is applied
Stress off
Stress on
Instant recovery (short times)
Permanent strain (deformation)
Instant strain
(short times)

## Slide 20
Statement often found in books: “viscoelastic materials
have Memory but this memory is a fadding memory, what
does it mean? The longer the time the less the material
“remembers its original configuration “Fadding memory”
Stress off
Stress on
Permanent strain
(deformation)
Experiment 1
Stress off
Stress on
Permanent strain
(deformation)
Experiment 2

## Slide 21
G
Maxwell Model
Two rheological Parameters
One Relaxation Time
Good “fadding” memory materials, e.g. dough
No as good fadding memory materials,
e.g. peanut butter
Perfect memory (any solid)
“Horrible” memory (any liquid, e.g. water)

## Slide 22
Behavior of a Maxwell Model when a “sudden”
constant strain is applied (Relaxation Test)
Relaxation Curve
G

## Slide 23
Behavior of a Maxwell Model when a “sudden”
constant strain is applied (Relaxation Test)
Relaxation Curves
G
tR decreases
Real Strain (Deformation)

## Slide 24
OTHER MODELS
Kelvin-Void Model (viscoelastic solid)

## Slide 25
CREEP TEST – CONSTANT LOAD
tret decreases
Retardation time
For Long Times
Small retardation time reaches
equilibrium quickly
Large retardation times reaches equilibrium slowly
Perfect solid

## Slide 26
MORE COMPLICATED MODELS
BURGER MODEL
(Good to describe ice cream)
What happens if we apply a constant
stress to the Burger’s model ?
Option 1 : Develop a mathematical model representing the system. Good
for modeling/simulation purposes
Option 2 : Do the test and try to get some meaningful parameters out of the
results

## Slide 27
BURGER’S MODEL
Instant Elastic
Deformation
Retarded Elastic
Deformation
Viscous
Flow
Instant
Recovery
Retarded
Recovery
Permanent
Deformation

## Slide 28
Step 1 – A sudden constant stress is applied
solid bar
solid bar
The only element acting is the spring 2 (G2)
Under a sudden stress the two dashpots act as solid bars. Short Time behavior
Instant deformation of spring 2 is:
BURGER’S MODEL

## Slide 29
BURGER’S MODEL
Retarded elastic response
Why the modulus of the spring 2 is not used
to describe the retarded elastic response ?
Step 2 What happens with the system after the stress has
been applied for some time ?

## Slide 30
BURGER’S MODEL
Step 3 What happens at long times ?
Why a linear response is observed ?
When a linear behavior starts ?
Why spring 2 does not participate in the curved part of the strain response?

## Slide 31
BURGER’S MODEL
Answers to Previous questions
Spring 1 will deform until reaches its equilibrium
strain for a given stress
After spring 1 reaches the equilibrium strain it will restrain
the deformation of dashpot 1
Spring 2 has been deformed initially
Only dashpot 2 will deform and the strain will be :
Straight line with slope

## Slide 32
BURGER’S MODEL
What happens when the stress is off?
Can Spring 2 recover its initial state?
What about Spring 1 ?

## Slide 33
BURGER’S MODEL
solid bar
solid bar
Off
Retarded
recovery

## Slide 34
Retarded
recovery
BURGER’S MODEL
Why only G1 and are acting in the retarded recovery of the system?
Answers
Spring 2 already reached its initial state (instant recovery)
Dashpot 2 will not further deform any longer because
Dashpot 1 is being unstrained for the recovery of spring 1, which is not instantaneous because is “retarded” by dashpot 1
Non-recoverable deformation (strain) is due to dashpot 2